## Slide 1: Calculating X-ray absorption spectra using RSPt
Felix Sorgenfrei
Uppsala University, Sweden

## Slide 2
Outline
Introduction
          Theoretical Methodology
          Applications
          Ferrites (Fe3O4, CoFe2O4, NiFe2O4)
Notes: Xray spectroscopy ….

## Slide 3
X-ray Absorption Spectroscopy (XAS)
Naming Scheme of edges
Continuum
Notes: Xray spectroscopy ….

## Slide 4
X-ray Absorption Spectroscopy (XAS)
Johan Schött: Theoretical and Computational Studies of Strongly Correlated Electron Systems
L3
L2
Ni site of NiFe2O4
Notes: Xray spectroscopy ….

## Slide 5
X-ray Magnetic Circular Dichroism (XMCD)
2p1/2
2p3/2
3d3/2
3d5/2
+ℏ (left)
Notes: Xray spectroscopy ….

## Slide 6
Element and angular momentum specific
XAS gives insight into electronic structure
XMCD gives insight into magnetic structrure
Importance of XAS & XMCD

## Slide 7
Our Approach: DFT+U+MLFT
840 850 860 870 880 890 900
Energy (eV)
0
1
2
3
4
5
6
7
Intensity (arb. units)
experiment theory
840 850 860 870 880 890 900
Energy (eV)
8
6
4
2
0
2
Intensity (arb. units)
experiment theory
XAS
XMCD
Ni
Ni
Theory
Experiment
NiFe2O4
Nearly parameter-free calculation of spectra with multiplet effects

## Slide 8
+ parameter free
+ detailed description of chemical structure
(DFT) only describes groundstate
(DFT) electron-electron correlations too simplified
DFT (+U / +DMFT)
XAS & XMCD
MLFT
(multi-configurational)
+ describes all many body effects
+ works well for localized systems
- strong parameter
dependence
MLFT: Multiplet Ligand Field Theory
Theoretical Methodology
Hybridization function

## Slide 9
Density Functional Theory
Calculate electron density
Calculate Potential
Construct DFT Hamiltonian
Solve for KS wavefunction
Non-interacting system (DFT)

## Slide 10
DMFT Loop
Dynamical Mean-Field Theory
Hybridization function
DFT Part
MLFT
yes
no

## Slide 11
Lattice Green’s function:
Local Green’s function:
Hybridization function:
U
U
U
U
U
U
U
U
U
U
t
t U
t U
t
Figure: Leonid Pourosvskii Nordita 2016
MLFT: generating impurity model

## Slide 12
MLFT: Hybridization function
Hybridization function:
Fitted hybridization function:
Energy (eV)

## Slide 13
with
MLFT: Impurity Hamiltonian
Calculated from first-principles
Fitted
Figure: Leonid Pourosvskii Nordita 2016
U
U
U
U
U
U
U
U
U
U
t
t U
t U
t

## Slide 14
with
MLFT: Spectra
Green’s Function
Spectral Function

## Slide 15
Fe Oh
Fe/Ni/Co Oh
Fe Td
(minority)
(majority)
(majority)
Fe (Td)
Fe (Oh)
O
Fe/Ni/Co (Oh)
Ferrites
3+
3+
2+

## Slide 16
XAS of Fe
L3
L2
Fe Oh
Fe Td
(minority)
(majority)
Fe Oh
(majority)
L3
L2
Fe3O4
Theory (80% Slater)
Experiment
XMCD of Fe
Theory (70-90% Slater)

## Slide 17
XAS
XMCD
Fe
Co
CoFe2O4
Theory (80% Slater)
Experiment
Theory (70-90% Slater)

## Slide 18
XAS
XMCD
Fe
Ni
NiFe2O4
Theory (80% Slater)
Experiment
Theory (70-90% Slater)

## Slide 19
XAS
XMCD
Fe
Ni
NiFe2O4: DMFT
LDA+U
Experiment
LDA+DMFT

## Slide 20
with
MLFT: Impurity Hamiltonian
Calculated from first-principles
Fitted
Figure: Leonid Pourosvskii Nordita 2016
U
U
U
U
U
U
U
U
U
U
t
t U
t U
t

## Slide 21
MLFT: Hubbard U and J
Notes: https://link.springer.com/article/10.1007/s00205-021-01692-x

## Slide 22
MLFT: Calculating the U matrix
radial
angular
Notes: https://link.springer.com/article/10.1007/s00205-021-01692-x

## Slide 23
MLFT: Calculating the U matrix
Angular part
Expectation value can be factorized into angular and radial part if separates
Depends only on Y
well known solution
Notes: https://link.springer.com/article/10.1007/s00205-021-01692-x

## Slide 24
MLFT: Calculating the U matrix
Radial part
Depends on radial part of
Called Slater integrals
Numerically evaluated
Notes: https://link.springer.com/article/10.1007/s00205-021-01692-x

## Slide 25
MLFT: Impurity Hamiltonian
Direct interaction
Exchange interaction
where , k = 0, 2, 4, … (k ≤ 2l) are multipole expansion coefficients
where , k = 1, 3, 5, … (k ≤ 2l) are multipole expansion coefficients
Notes: https://link.springer.com/article/10.1007/s00205-021-01692-x

## Slide 26
MLFT: Screening at the L-edge
Notes: https://link.springer.com/article/10.1007/s00205-021-01692-x

## Slide 27
cDFT: Calculation of

## Slide 28
cDFT: Calculation of

## Slide 29
Results
Compound |  |  |  | 
 | Calculated | Ref. [1] | Calculated | Ref. [1]
FeO | 5.34 | 6.50 | 7.55 | 7.50
NiO | 7.21 | 7.50 | 8.73 | 8.90
Compound |  |  |  | 
 | Calculated | Ref. [1] | Calculated | Ref. [1]
FeO | 5.34 | 6.50 | 7.55 | 7.50
NiO | 7.21 | 7.50 | 8.73 | 8.90
[1] Fitted by Lüder et al. 2017

## Slide 30
80% of bare value
70% of bare value
NiFe2O4: Influence of
90% of bare value
XAS
XMCD

## Slide 31
NiFe2O4: Influence of
+ 1 eV
+ 0.5 eV
XAS
XMCD

## Slide 32
MLFT: Double Counting
The Es are averaged over all possible states

## Slide 33
MLFT: Double Counting
parameter
Shifts energy of the ligands
Spin independent (no exchange)
LSDA can lead to weird branching ratios
Use LDA instead

## Slide 34
Nearly parameter-free calculation of spectra with multiplet effects
Calculates XAS branching ratios correctly
Works well for strongly localized and hybridized systems
Conclusion
840 850 860 870 880 890 900
Energy (eV)
0
1
2
3
4
5
6
7
Intensity (arb. units)
experiment theory
840 850 860 870 880 890 900
Energy (eV)
8
6
4
2
0
2
Intensity (arb. units)
experiment theory
XAS
XMCD
Ni
Ni
Theory
Experiment
NiFe2O4